# INLAND ATOMIZE METAL POWDER LLP

Survey No. 230/2, Por-Mangej Road, Village - Manglej, Ta. KARJAN, Vadodara - 391243

Email:lnfo@lnlandatomlzemetalpowderllp. com

Mo: +9196623 00876

Tin (Sn) Powder

IAMP is specialist to supply Tin powders by VIGA process, which meet specific technical requirements such as Apparent Density, Specific Surface Area and Purity.

Physical Properties of Tin powder:

| Molecular Formula: | Sn | Color: | Grey silvery powder |
| --- | --- | --- | --- |
| Shape: | Spherical form | Purity: | 99.95% |
| Product method: | Gas atomized | Molecular Weight: | 118.69 |
| Freezing/Melting Point: | 231.9-233℃ | Boiling Point: | 2270 ℃ |
| Specific Gravity/Density: | 7.31g/cm3 | Applicable Solubility in water: | Slightly soluble in hot water. |

Applications:

- Powder Metallurgy (P/M): Used in pressed and sintered components such as self-lubricating bronze bearings, bushings, and filters.

- Metallurgical & Chemical Reaction: Coarse grades are used.

- Advanced Material Applications: Fine grades are used in diamond tools, solder pastes, electrically conductive polymers, and metal matrix composites.

- Surface Engineering: Applied in thermal spray coatings, cold spray, and sintered overlays for wear resistance and corrosion protection.

- Joining Technologies: Incorporated in brazing pastes, soft solders, and fluxes for precision joining of copper, aluminium, and specialty alloys.

- Miscellaneous: Used in friction materials (e.g., brake pads), decorative coatings, and radiation shielding due to its high density and corrosion resistance.

Specification:

| Grade | Composition (%) | A.D.g/cm3 | Particle Size |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | +100(150μm) | +140(106μm) | +200(75μm) | +325(45μm) | -325(45μm) |
| IAMP – Sn 100 | Sn 99.9min | 3.0-3.8 | ≤5 | Bal. |  |  | ≤10 |
| IAMP – Sn 200 |  |  | - | ≤1 | ≤5 | ≤30 | Bal. |
| IAMP – Sn 300 |  |  | - | - | ≤1 | ≤10 | Bal. |

Packaging:

Tin powder will be supplied by standard packing in Vacuum bag of 5Kg, 10Kg, and 25Kg or can be supplied as per customer special requirement.

Storage:

Tin powders oxidation more easily, especially in the moist air to oxidation.

It should be packing in a cool and dry plastic bags filled with inert gas or protection in the tank